Overview: The EZ MIX PAK is a rectangular, clear, two-component package containing Aptek materials. The EZ MIX PAK consists of parts A and B and is separated by a burstable seam in the middle of the pack. The convenient EZ MIX PAKS are designed to eliminate the need for accurate weighing equipment – i.e. scales, cups, spatulas, etc.

STEP # 1:  Cut the brown, foil-lined, outer package and remove the EZ MIX PAK. (Refer to picture for STEP # 1)

STEP # 2: Inspect the EZ MIX PAK. If there is any leakage noted, do not use. NOTE: If one or both sides of the material in the EZ MIX PAK contain filler, then filler/resin separation may be noted. If any separation has occurred on one or both sides of the EZ MIX PAK, homogenize the material by mixing the separated side by hand, using thumbs and opposing fingers to knead material to uniform consistency.

STEP # 3:  Hold the EZ MIX PAK with both hands, one at either end of the package. Note if a packet on either side of the barrier is unequal in length or volume (Refer to picture of STEP # 2). If so, then the contents of the smaller side must initially be forced into the larger side to start the mixing process.

STEP # 4:  Mixing process: Using a sharp, 90º angled, cornered surface of a table or work bench, slowly press the EZ MIX PAK against the corner of the table, forcing the liquid of one side, to burst the barrier, and to enter into the other side of the EZ MIX PAK.  (Refer to pictures for STEP # 3)

STEP # 5:  Continue to mix both parts together by dragging the EZ MIX PAK from top to bottom against the sharp surface. Be sure to move the material up and down the EZ MIX PAK to ensure thorough mixing. (Refer to pictures for STEP # 5a). You may need to intermittently knead the mix by hand as well to aid in the mixing process (Refer to picture for STEP # 5b).  It will take a couple minutes to fully mix the material. Continue mixing until the mixture is uniform.

STEP # 6:  Once the material looks uniform in color and consistency, cut the corner of the EZ MIX PAK and extrude into a dish or use as needed. (Refer to picture for STEP # 6). NOTE: Aptek has made all efforts to eliminate air from this system. However, because of the need for argon/nitrogen in the material to maintain stability and to allow for proper mixing action, some air will remain in the system after mixing. To obtain a void-free mixture, transfer material into container and de-gas this material until break.

NOTE:  Pictures correspond with written instructions to the left.

STEP # 1                            STEP # 2                            STEP # 3

→    →

STEP # 4

→→→

STEP # 5a

→→→

STEP # 5b                                     STEP # 6

→